# Application No.:  379736

# Equipment Category – Aluminum Melting Furnace

| 1. GENERAL INFORMATION |  | DATE: 4/15/2003 |
| --- | --- | --- |
| a. manufacturer: Thorpe Industrial Furnace |
| b. type: Reverbatory | c. model: |
| d. style: Has recuperator (810F air temperature to burners) |
| e. applicable aqmd rules: 2012 |
| f. cost: $ () source of cost data: |
| g. operating schedule: 24 hrs/day 5 days/wk 50 wks/yr |

| 2. EQUIPMENT INFORMATION |  | App. No.: 379736 |
| --- | --- | --- |
| A. FUNCTION: RECLAIM device No. D2: melts prime aluminum (from primary foundaries) and house scrap. |
| B. maximum Heat Input: 12.8 MMBtu/hr | C. maximum throughput: 120 tpd (typical) |
| D. burner information: no.: 2 type: Low-NOx |
| e. primary fuel: Natural Gas | f. other fuel: None |
| g. operating conditions: Batch operation. Batch size is approximately 40 tons. Typically, three batches per day. |

| 3. COMPANY INFORMATION |  | App. No.: 379736 |
| --- | --- | --- |
| A. NAME: International Extrusion Corp. | B. SIC CODE: 3354 |
| C. ADDRESS: 1000 Meridian Ave. CITY: Alhambra STATE: CA ZIP: 91803 |
| D. CONTACT PERSON: Bob Olivas | E. PHONE NO.: 626-576-2424 |

| 4. PERMIT INFORMATION |  | App. No.: 379736 |
| --- | --- | --- |
| A. AGENCY: SCAQMD | B. application type: |
| C. AGENCY CONTACT PERSON: Manny Quizon | D. PHONE NO.: 909-396-2639 |
| E. PERMIT TO CONSTRUCT/OPERATE INFORMATION: P/C NO.: 379736 ISSUANCE DATE: 3/29/2001 check if no p/c P/O NO.: 379736 ISSUANCE DATE: 2/15/2002 |
| F. START-UP DATE: 3/29/2001 |

| 5. EMISSION INFORMATION |  | App. No.: 379736 |
| --- | --- | --- |
| A. PERMIT |
| A1. PERMIT LIMIT: NOx not to exceed 37 ppmvd@3%O2 (RECLAIM Concentration Limit) |
| A2. bact/lAer DETERMINATION: 37 ppmvd@3%O2 (low-NOx burner) |
| a3. BASIS OF THE BACT/LAER DETERMINATION: Achieved in Practice |
| B. CONTROL TECHNOLOGY |
| B1. MANUFACTURER/SUPPLIER: Bloom Engineering Co. |
| B2. TYPE: Low-NOx Burner |
| B3. DESCRIPTION: Model 1630-LXX, 6.4 MMBtu/hr |
| B4. CONTROL EQUIPMENT PERMIT APPLICATION DATA: P/C NO.: ISSUANCE DATE: P/O NO.: ISSUANCE DATE: |
| B5. WASTE AIR FLOW TO CONTROL EQUIPMENT: FLOW RATE: ACTUAL CONTAMINANT LOADING: BLOWER HP: |
| B6. WARRANTY: NOx guaranteed not to exceed .04 lb/MMBtu (32 ppmvd@3%O2) |
| B7. PRIMARY POLLUTANTS: NOx, CO, VOC, PM |
| B8. SECONDARY POLLUTANTS: |
| B9. SPACE REQUIREMENT: |
| B10. LIMITATIONS: | B11. UNUSED |
| B12. OPERATING HISTORY: |
| B13. UNUSED | B14. UNUSED |
| C. CONTROL EQUIPMENT COSTS |
| C1. CAPITAL COST: check if installation cost is included in EQUIPMENT cost EQUIPMENT: $ INSTALLATION: $ () SOURCE OF COST DATA: |
| C2. ANNUAL OPERATING COST: $ () SOURCE OF COST DATA: |
| D. DEMONSTRATION OF COMPLIANCE |
| D1. STAFF PERMFORMING FIELD EVALUATION: ENGINEER'S NAME: INSPECTOR'S NAME: DATE: |
| D2. COMPLIANCE DEMONSTRATION: |
| D3. VARIANCE: NO. OF VARIANCES: None DATES: CAUSES: |
| D4. VIOLATION: NO. OF VIOLATIONS: None DATES: CAUSES: |
| D5. MAINTENANCE REQUIREMENTS: | D6. UNUSED |
| D7. SOURCE TEST/PERFORMANCE DATA RESULTS AND ANALYSIS: DATE OF SOURCE TEST: 9/52001 CAPTURE EFFICIENCY: DESTRUCTION EFFICIENCY: OVERALL EFFICIENCY: SOURCE TEST/PERFORMANCE DATA: Temperatures, F ppmvd@3%O2 Furnace % Load Roof Exhaust O2, % (dry) NOx CO D2 (Melting) 30 1850 423 15.3 31.7 <1 100 1900 439 13.0 31.0 <1 OPERATING CONDITIONS: Test durations were 30 minutes at each load. TEST METHODS: AQMD Method 100.1. Test was approved by AQMD Monitoring & Source Test Engineering group. |

| 6. COMMENTS |  | App. No.: 379736 |
| --- | --- | --- |
| This is a RECLAIM facility. The facility requested a permit modification to apply a RECLAIM concentration limit of 37 ppmvd (corrected to 3% O2) to this furnace. This low-NOx burner is considered achieved in practice. Although this burner is capable of meeting a NOx limit of 37 ppm in this furnace when operated on natural gas, NOx emissions may be different in other furnaces with other burner/furnace configurations, operating temperatures or other operating conditions. It is suggested the the NOx emission guarantee or 60 ppm, the BACT Part D guideline, be used as a starting point in permitting a new or modified furnace, i.e., in the Permit to Construct, and that the final NOx limit in the Permit to Operate be determined after source testing is completed. Source testing should include the highest-NOx operating mode |