Application No.:  322398

Equipment Category – Dryer or Oven

| 1. GENERAL INFORMATION |  | DATE: 11/27/2002 |
| --- | --- | --- |
| a. manufacturer: Unknown |
| b. type: Conveyorized, three-zone, 8-layer | c. model: |
| d. style: |
| e. applicable aqmd rules: None |
| f. cost: $ () source of cost data: |
| g. operating schedule: 24 hrs/day 5 days/wk 50 wks/yr |

| 2. EQUIPMENT INFORMATION |  | App. No.: 322398 |
| --- | --- | --- |
| A. FUNCTION: Facility manufactures perlite thermal/acoustical insulation board used mainly for roofing. Continuous 8.5 ft-wide board is formed from slurry in standard thicknesses from 1/2" to 1". This drying oven is the last process step before cutting board to lengths. The three dryer zones have the following burners and maximum operating temperatures: Zone 1 - two 16 MMBtu/hr burners (650F), Zone 2 - two 20 MMBtu/hr burners (650F), Zone 3 - two 12 MMBtu/hr burners (500F). |
| B. maximum Heat Input: 96 MMBtu/hr | C. maximum throughput: 5,000 lb/hr perlite ore (normal operating rate) |
| D. burner information: no.: 6 type: Eclipse Minnox |
| e. primary fuel: Natural Gas | f. other fuel: |
| g. operating conditions: Continuous, steady |

| 3. COMPANY INFORMATION |  | App. No.: 322398 |
| --- | --- | --- |
| A. NAME: BMCA Insulation Products | B. SIC CODE: 2961 |
| C. ADDRESS: 300 N. Haven Avenue CITY: Ontario STATE: CA ZIP: 91761 |
| D. CONTACT PERSON: Facility Closed | E. PHONE NO.: |

| 4. PERMIT INFORMATION |  | App. No.: 322398 |
| --- | --- | --- |
| A. AGENCY: SCAQMD | B. application type: |
| C. AGENCY CONTACT PERSON: Manuel Quizon | D. PHONE NO.: 2639 |
| E. PERMIT TO CONSTRUCT/OPERATE INFORMATION: P/C NO.: 322398 (A/N) ISSUANCE DATE: 1/2/1997 check if no p/c P/O NO.: 322398 (A/N) ISSUANCE DATE: 9/11/1998 |
| F. START-UP DATE: January 1997 -- expected by applicant at time of application (Nov 1996). |

| 5. EMISSION INFORMATION |  | App. No.: 322398 |
| --- | --- | --- |
| A. PERMIT |
| A1. PERMIT LIMIT: 6 ppm NOx at 15% O2, 2000 ppm CO, 0.1 grain/SCF natural gas |
| A2. bact/lAer DETERMINATION: Above NOx limit was requested by the applicant, based on the results of a source test, to make the dryer super-compliant for RECLAIM. |
| a3. BASIS OF THE BACT/LAER DETERMINATION: |
| B. CONTROL TECHNOLOGY |
| B1. MANUFACTURER/SUPPLIER: Eclipse |
| B2. TYPE: Low-NOx burners |
| B3. DESCRIPTION: Model No.s 5625, 4625, 3500 |
| B4. CONTROL EQUIPMENT PERMIT APPLICATION DATA: P/C NO.: ISSUANCE DATE: P/O NO.: ISSUANCE DATE: |
| B5. WASTE AIR FLOW TO CONTROL EQUIPMENT: FLOW RATE: ACTUAL CONTAMINANT LOADING: BLOWER HP: |
| B6. WARRANTY: Eclipse guaranteed 10 ppm NOx and 50 ppm CO (uncorrected) |
| B7. PRIMARY POLLUTANTS: NOx, CO, VOC, SOx, PM10 |
| B8. SECONDARY POLLUTANTS: |
| B9. SPACE REQUIREMENT: |
| B10. LIMITATIONS: | B11. UNUSED |
| B12. OPERATING HISTORY: The equipment operated from early 1997 until the facility shut down in November 1998. |
| B13. UNUSED | B14. UNUSED |
| C. CONTROL EQUIPMENT COSTS |
| C1. CAPITAL COST: check if installation cost is included in EQUIPMENT cost EQUIPMENT: $ INSTALLATION: $ () SOURCE OF COST DATA: |
| C2. ANNUAL OPERATING COST: $ () SOURCE OF COST DATA: |
| D. DEMONSTRATION OF COMPLIANCE |
| D1. STAFF PERMFORMING FIELD EVALUATION: ENGINEER'S NAME: INSPECTOR'S NAME: DATE: |
| D2. COMPLIANCE DEMONSTRATION: |
| D3. VARIANCE: NO. OF VARIANCES: DATES: CAUSES: |
| D4. VIOLATION: NO. OF VIOLATIONS: DATES: CAUSES: |
| D5. MAINTENANCE REQUIREMENTS: | D6. UNUSED |
| D7. SOURCE TEST/PERFORMANCE DATA RESULTS AND ANALYSIS: DATE OF SOURCE TEST: October 9 and 31, 1997 CAPTURE EFFICIENCY: DESTRUCTION EFFICIENCY: OVERALL EFFICIENCY: SOURCE TEST/PERFORMANCE DATA: Test 1" Board (10/9/97) 1/2" Board (10/31/97) 3/4" Board (10/31/97) Dryer Zone 1 2 3 1 2 3 1 2 3 Temperature, F 262 405 193 295 376 289 282 407 226 NOx (ppmvd@15%O2) 0.42 2.3 0.16 1.3 0.91 2.3 1.2 1.0 3.8 CO (ppmvd@15%O2) 19 63 41 34 8.7 106 24 6.5 141 OPERATING CONDITIONS: TEST METHODS: This source test was reviewed and accepted by AQMD's Monitoring and Source Test Engineering group. |

| 6. COMMENTS |  | App. No.: 322398 |
| --- | --- | --- |
| The low-NOx burners used in this case are considered achieved in practice for ovens and dryers. Although these burners are capable of meeting a NOx limit of 6 ppmvd, corrected to 15% O2, in this oven, NOx emissions may be different in other ovens/dryers with other burner/furnace configurations, operating temperatures or other operating conditions. Although a NOx guarantee of 10 ppm (uncorrected) was provided by the burner manufacturer in this case, the NOx emission level guaranteed will depend on the design and operational characteristics of the oven or dryer. It is suggested the the NOx emission guarantee or the BACT Part D guideline be used as a starting point in permitting a new or modified oven or dryer, i.e., in the Permit to Construct, and that the final NOx limit in the Permit to Operate be determined after source testing is completed. Source testing should include the highest-NOx operating mode. |