Application No.:	  N-2253-18-2

Equipment Category – Flow Coater

| 1. general information |  | DATE: 5/13/2003 |
| --- | --- | --- |
| a. manufacturer: Crabtree at Gateshead, Ltd. |
| b. type: Sheet Coater | c. model: 13X45-F1 |
| d. style: With attached UV curing oven |
| e. applicable aqmd rules: NA |
| f. cost: $ () source of cost data: |
| g. operating schedule: 24 hrs/day 7 days/wk 52 wks/yr |

| 2. EQUIPMENT INFORMATION |  | App. No.: N-2253-18-2 |
| --- | --- | --- |
| A. FUNCTION: Used to apply exterior coatings to sheets used for can manufacture. |
| b. size/dimension/capacity: 80 sheets/minute (sheets are approx. 3' x 3') |
| c. blowers: | d. total flow rate: scfm |
| e. material stored/processed/handled: |
| f. throughput/process rate/usage rate: 80 sheets/minute |

| 3. COMPANY INFORMATION |  | App. No.: N-2253-18-2 |
| --- | --- | --- |
| A. NAME: Ball Western Can Co. | B. SIC CODE: 3411 |
| C. ADDRESS: 300 W. Gregor Street CITY: Oakdale STATE: CA ZIP: 95361 |
| D. CONTACT PERSON: Bob Hall | E. PHONE NO.: 303-460-5445 |

| 4. PERMIT INFORMATION |  | App. No.: N-2253-18-2 |
| --- | --- | --- |
| A. AGENCY: SJVAPCD | B. application type: |
| C. AGENCY CONTACT PERSON: Mark Schonhoff | D. PHONE NO.: 209-557-6448 |
| E. PERMIT TO CONSTRUCT/OPERATE INFORMATION: P/C NO.: N-2253-18-2 ISSUANCE DATE: 10/7/2001 check if no p/c P/O NO.: ISSUANCE DATE: |
| F. START-UP DATE: June 2001 |

| 5. EMISSION INFORMATION |  | App. No.: N-2253-18-2 |
| --- | --- | --- |
| A. PERMIT |
| A1. PERMIT LIMIT: Facility has annual, quarterly and daily VOC emission caps. |
| A2. bact/lAer DETERMINATION: UV coating system equivalent to or exceeding 95% overall control of VOC. |
| A3. BASIS OF THE BACT DETERMINATION: Achieved in practice |
| B. CONTROL TECHNOLOGY |
| B1. MANUFACTURER/SUPPLIER: Crabtree at Gateshead, Ltd. |
| B2. TYPE: UV cured sheet coater |
| B3. DESCRIPTION: This sheet coater employs a UV-curable coating material. The coated metal sheets leaving the sheet coater enter a UV curing section, where the coating is exposed to UV light. The chemical nature of the coating material causes it to harden due to cross-linking reactions that are initiated by the UV light. Unlike conventional oven curing, this process releases no measureable VOC, and is vented directly to the atmosphere. |
| B4. CONTROL EQUIPMENT PERMIT APPLICATION DATA: P/C NO.: ISSUANCE DATE: P/O NO.: ISSUANCE DATE: |
| B5. WASTE AIR FLOW TO CONTROL EQUIPMENT: FLOW RATE: ACTUAL CONTAMINANT LOADING: .) BLOWER HP: |
| B6. WARRANTY: |
| B7. PRIMARY POLLUTANTS: VOC |
| B8. SECONDARY POLLUTANTS: |
| B9. SPACE REQUIREMENT: |
| B10. LIMITATIONS: | B11. UNUSED |
| B12. OPERATING HISTORY: The equipment has been in regular service since startup. |
| B13. UNUSED | B14. UNUSED |
| C. CONTROL EQUIPMENT COSTS |
| C1. CAPITAL COST: check if installation cost is included in capital cost EQUIPMENT: $ INSTALLATION: $ () SOURCE OF COST DATA: |
| C2. ANNUAL OPERATING COST: $ () SOURCE OF COST DATA: |
| D. DEMONSTRATION OF COMPLIANCE |
| D1. STAFF PERMFORMING FIELD EVALUATION: ENGINEER'S NAME: INSPECTOR'S NAME: DATE: |
| D2. COMPLIANCE DEMONSTRATION: |
| D3. VARIANCE: NO. OF VARIANCES: DATES: CAUSES: |
| D4. VIOLATION: NO. OF VIOLATIONS: DATES: CAUSES: |
| D5. MAINTENANCE REQUIREMENTS: | D6. UNUSED |
| D7. SOURCE TEST/PERFORMANCE DATA RESULTS AND ANALYSIS: DATE OF SOURCE TEST: CAPTURE EFFICIENCY: DESTRUCTION EFFICIENCY: OVERALL EFFICIENCY: SOURCE TEST/PERFORMANCE DATA: OPERATING CONDITIONS: TEST METHODS: |

| 6. COMMENTS |  | App. No.: N-2253-18-2 |
| --- | --- | --- |
| Permit to Operate is in process. The facility contact estimates that use of a conventional coating method would have released approximately 2,300 lb/day to the VOC control system. For cans used for foodstuffs, UV-curable coating materials can be used for coating of can exteriors, but have not been approved for can interiors. |